









T E C H N I C A L	D A T A	S H E E T

SAC0307 Lead Free SOLDER WIRE

PRODUCT DESCRIPTION

SAC0307 RoHS Compliance Solder Wires are being formulated with High Virgin Raw Metals Processed in state-of-the-art Technology that brings world class Quality along. Here, Oxygen interaction with Alloy is Nil and thus, Dross formulation is reduced at PCB Assembly Process. Also an increase flow rate & reduced impurities found. SAC0307 Alloy is compatible for a typical range of Flux Application Formulas used in Electronics Industry Today.

STORAGE AND HANDLING

· Do not use Fire near storage area.
· Store in Dry, Cool and Non-Corrosive environment.
· Wear Personal Protective Equipments while Handling.
· Wear Personal Protective Equipments while Processing.

PRODUCT SPECIFICATION


	Sl No
	Item
	Specification
	Standard

	1
	Appearance
	Bright and shiny surface finishes
	

	2
	Alloy
	Sn/Ag0.3/Cu0.7/Ni0.06/Ge0.01
	JIS-Z-3282 A CLASS

	3
	Melting Point
	217~2260C
	DSC

	4
	Flux Content
	2.0 ±0.2 % NC flux
	JIS-Z-3283

	5
	Halide Content Under
	0.1%
	JIS-Z-3283

	6
	Gravity
	7.4
	

	7
	Spread ability
	> 80%
	JIS-Z-3197

	8
	Packaging
	500g,
	

	9
	Diameter/Tolerance
	0.7mm,1.2mm & 1mm ± 0.02 mm
	JIS-Z-3283

	10
	Flux Type
	ROL0
	J-STD-004

	11
	RoHS Complaint
	Yes
	International Standards

	12
	Features
	Excellent solder joint reliability. Superior joint strength.
Excellent thermal & Mechanical fatigue resistance. Low cleaning required after solder joint

	13
	Purpose
	For use in applications requiring good activation.





.



PHYSICAL PROPERTIES.

	No
	Test Item
	Test Result
	Test Method

	1
	Silver Chromate Test
	PASS
	IPC-TM-650, 2.6.33

	2
	Copper Mirror Test
	PASS
	IPC-TM-650, 2.6.32

	3
	Copper plate Corrosion
	PASS
	JIS-Z-3197, 6.6.1

	4
	S.I.R Test
	1×109 up
	IPC-TM-650, 2.6.3.3

	5
	Electro migration Test
	1×10912up
	IPC-TM-650, 2.6.14.1




ALLOY COMPOSITION.

	(Sn)
	(Ag)
	(Cu)
	(Ni)
	(Ge)
	(Zn)
	(Al)
	(Sb)
	(Fe)
	(As)
	(Bi)
	(Cd)
	(Pb)

	REM.
	0.2~
0.4
	0.6~
0.8
	0.01
MAX
	0.005~
0.02
	0.002
MAX
	0.002
MAX
	0.12
MAX
	0.02
MAX
	0.03
MAX
	0.10
MAX
	1
PPM
	100
PPM







































