T E C H N I C A L	D A T A	S H E E T

T E C H N I C A L	D A T A	S H E E T

Sn99.3Cu0.7 Lead Free Solder Wire

## PRODUCT DESCRIPTION

Sn99.3Cu0.7 RoHS compliance solder wires are being formulated with virgin raw metals processed in state-of-the-art Technology that brings world class quality along. Here, oxygen interaction with alloy is nil and thus, dross formulation is reduced at PCB assembly process. Also an increased flow rate & reduced impurities found. Sn99.3Cu0.7 alloy is compatible for a typical range of flux application formulas used in Electronics Industry today.

## STORAGE AND HANDLING

- Do not use fire near storage area.

- Store in dry, cool and non-corrosive environment.

- Wear Personal Protective Equipments while handling.

- Wear Personal Protective Equipments while processing.

## PRODUCT SPECIFICATION

| Sl No | Item | Specification | Standard |
| --- | --- | --- | --- |
| 1 | Appearance | Bright and shiny surface finishes |  |
| 2 | Alloy | Sn99.3Cu0.7 | JIS-Z-3282 A CLASS, ISO9453 |
| 3 | Melting Point | 227°C | DSC |
| 4 | Flux Content | 1.5%,2%,2.2% & 2.3% ±0.2 % NC flux | JIS-Z-3283 |
| 5 | Halide Content Under | 0.05% | J-STD-004 |
| 6 | Gravity | 7.4gm/cm³ at 20°C |  |
| 7 | Spread ability | > 80% | JIS-Z-3197 |
| 8 | Packaging | 500gm |  |
| 9 | Diameters / Tolerances | 16SWG,18SWG,20SWG,22SWG,24 SWG & 26 SWG | JIS-Z-3283 |
| 10 | Flux Type | ROL0 | J-STD-004 |
| 11 | Shelf Life | 5 Years | NA |
| 12 | RoHS Complaint | Yes | International Standards |
| 13 | Features | Excellent solder joint reliability. Superior joint strength. Excellent thermal & Mechanical fatigue resistance. |  |
| 14 | Purpose | For use in applications requiring good activation. |  |

## PHYSICAL PROPERTIES.

| No | Test Item | Test Result | Test Method |
| --- | --- | --- | --- |
| 1 | Silver Chromate Test | PASS | IPC-TM-650, 2.6.33 |
| 2 | Copper Mirror Test | PASS | IPC-TM-650, 2.6.32 |
| 3 | Copper plate Corrosion | PASS | JIS-Z-3197, 6.6.1 |
| 4 | S.I.R Test | 1×109 up | IPC-TM-650, 2.6.3.3 |
| 5 | Electro migration Test | 1x1012 up | IPC-TM-650, 2.6.14.1 |

## ALLOY COMPOSITION:

| (Sn) | (Cu) | (Zn) | (Al) | (Sb) | (Fe) | (As) | (Bi) | (Cd) | (Pb) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| REM. | 0.6~ 0.8 | 0.001 MAX | 0.001 MAX | 0.10 MAX | 0.02 MAX | 0.03 MAX | 0.10 MAX | 1 PPM | 100 PPM |