[image: image1.jpg]



[image: image2.jpg]RIEDER

Rieder Sales GmbH | GlemmerstraBe 2115751 Maishofen | Austria

+43 6542 690 844 Landesgericht Salzburg Geschaftsfuhrung Bank fur Tirol und Vorarlberg AG
office@rieder.cc FN 483402 k Wolfgang Rieder BIC BTVAAT22
www.rieder.cc UID Nr. ATU 72859123 IBAN AT21 1643 0001 4319 0579




[image: image3.jpg]Rieder Smart Elements GmbH | Miihlenweg 22 | 5751 Maishofen | Austria

+43 6542 690 844 Landesgericht Salzburg Geschaftsfihrung Bank furTirol und Vorarlberg
office@rieder.cc FIN189909d Wolfgang Rieder BIC BTVAATZZ
www.rieder.cc UIDNr ATUB1557005 Angelika Rieder IBAN ATS7 16430001 4316 9367





Tender specification formparts
Formed glassfibre reinforced concrete panels for facade cladding

Status: April 2024
General
Information in the text of the invitation for tender must be reviewed and, if necessary, supplemented for the object.
Further liability by Rieder Smart Elements GmbH & Co KG is excluded. This also applies to printing and writing mistakes and to any subsequent changes. The respective national laws, standards and preliminary remarks for advanced rear-ventilated façades amended from time to time shall apply.
Loading, storage and handling provisions of the manufacturer must be observed.
General construction technique permit 

Glassfibre reinforced concrete panels "fibreC" to cover exterior walls are certified with a general construction technique permit (allgemeine Bauartgenehmigung) “Z-31.4-166". 
Certificate of conformance Austria

Austrian Certificate of Conformance No.: Z-6.1.2-04-4772

fibreC formparts 









__________________ rm
Technical material description
· fibreC glassfibre reinforced concrete panels produced of mineral raw materials
· Production method by extrusion
· Reinforcement by alkaline-resistant glass fibres in the matrix (CEM-Fil, approval Z-3.72-1731), 2-layer textile glass fabric (each longitudinally and cross-wise) and short fibres 
· Continuous colouration of the entire panel. Liquid dyes for colouration of the cement-bound building materials correspond to DIN EN 12878. The pigments used in the liquid dyes are light-, UV- and weather-resilient and not solvable in water, alkalines or diluted acids.
· Building material class A1 not flammable pursuant to DIN 4102 | EN 13501
· Manufacturer certification: ISO 14001:2009 and ISO 9001:2008 
· Crystalline silica < 0% - not detectable 

· Surface protection: The surface is applied with a transparent hydrophobic coating by default.
Sizes

· Standard panel dimensions 2,500 x 1,310 mm, 3,100 x 1,310 mm, 3,600 x 1,310 mm special sizes on request
· Dimension deviation length (3.6 m)
± 3 mm
EN 12467
· Dimension deviation width (1.2 m)
± 2 mm
EN 12467
· Diagonal difference up to 1.5 m | above 1.5 m ± 3.5 mm | ± 4 mm DIN 18202
· Diagonal difference as of 2.5 m | above 3.6 m ± 5 mm | ± 6 mm DIN 18202
· Thickness 13 mm 
· Thickness tolerance ± 10 % EN 12467
· Edge straightness (level 1)
± 0.1 %
EN 12467
· Rectangularity (level 1)
± 2 mm/m
EN 12467
Physical properties
· Tolerances of plan system up to 0.6 | up to 1.2 | up to 3.6 m  ± 2 mm | ± 4 mm | ± 8 mm DIN 18202
· Swelling size 0.384 mm/m
· Shrinkage size 0.737 mm/m
· Raw density (13 mm) 2.0 - 2.42 kg/dm³ EN 12467
· Bending tensile resilience > 18 N/mm² (MOR*) EN 12467, class 4
· E-modus for deformation calculation approx. 10,000 N/mm²
· E-modus for compression calculation approx. 30,000 N/mm²
· Dead weight / area weight (13 mm) 26 - 31.5 kg/m² depending on shade
· Heat expansion coefficient 10*10^(-6) 1/°k DIN 51045
· Building material class (panel | system) A1-not flammable | A2-s1,d0 - not flammable DIN 4102 | EN 13501-1
· Temperature stability depending on core moisture up to 350° 
· Specific heat capacity approx. 1,000 Joule / (kg*K)
· Heat conductivity lambda: approx. 2.0 W / (m*K)
· Moisture expansion ± 0.05 % EN 12467
Weather resilience
· Water impermeability passed EN 12467
· Heat-rain alternating test passed EN 12467
· Frost resistance passed EN 12467
· Frost-thaw alternating test
passed EN 12467
· UV-light resilience DIN 12878
· Wet storage resilience passed EN 12467
· Hot-water resilience passed EN 12467
** MOR: Modus of Rupture; design values deviate from MOR according to national provisions. The national approvals and provisions on calculation of the rated resistance shall apply
Packed weather-tightly on pallets. Loading, storage and handling provisions of the manufacturer must be observed.
Ventilated façade covers on existing substructure according to technical provisions and applicable standards.
Supplier of formparts:
Rieder Smart Elements GmbH & Co KG



Gemmerstraße 21, 5751 Maishofen, Österreich




T +43 6542 690 844, office@rieder.cc, www.rieder.cc

COLOURS
Colour collection greyscale:

polar white 



_____________ rm
off-white 



_____________ rm
ivory 



_____________ rm
silvergrey 



_____________ rm
chrome 



_____________ rm
anthracite 



_____________ rm
liquid black 



_____________ rm
Colour collection bricky:

coralline



_____________ rm
terracotta 



_____________ rm
oxide red



_____________ rm
burgundy



_____________ rm
merlot



_____________ rm
Colour collection timber:

larch



_____________ rm
oak




_____________ rm
walnut



_____________ rm
ebony



_____________ rm
terra



_____________ rm
Colour collection pietra:

cotton



_____________ rm
vanilla



_____________ rm
sahara



_____________ rm
sandstone



_____________ rm
almond



_____________ rm
Other Colours:

green



_____________ rm
SURFACE formparts sharp-edged
ferro: sandblasted surface

ferro light: slightly sandblasted surface
matt: smooth, brushed surface
SURFACE formparts round-edged

ferro: sandblasted surface

ferro light: slightly sandblasted surface (on request)
Special Textures Formparts sharp-edged
terrazzo black ferro plus

_____________ rm
vintage matt



_____________ rm
groove ferro soft


_____________ rm
groove ferro light


_____________ rm
groove ferro



_____________ rm
twine ferro soft


_____________ rm
twine ferro light


_____________ rm
twine ferro



_____________ rm
salt’n’pepper ferro plus

_____________ rm
salt’n’pepper ferro


_____________ rm
luce silver ferro


_____________ rm
lumber ferro



_____________ rm
slate ferro soft


_____________ rm
special textures Formparts round-edged
salt’n’pepper ferro plus

_____________ rm
salt’n’pepper ferro


_____________ rm
luce silver ferro


_____________ rm
FORMPARTS

[image: image3.jpg]U-shape: 






_______________pcs.
Edge


rounded 
sharp
Length in mm

_____________________________
Back in mm 

_____________________________
Leg 1 in mm

_____________________________
Leg 1 angle in °

_____________________________
Leg 2 in mm

_____________________________
Leg 2 angle in °

_____________________________
Diagonal cuts according to drawing no.___________________
Mitre cuts according to drawing no.
______________________
L-shape:






 _______________pcs.
Edge


rounded 
sharp
Length in mm

_____________________________
Back in mm 

_____________________________
Leg 1 in mm 

_____________________________
Leg 1 angle in ° 

_____________________________
Diagonal cuts according to drawing no ___________________
Mitre cuts according to drawing no_______________________
Round arc: 






_______________pcs.
Unwinding length x unwinding width: ____________________
Radius: ___________°
SERVICE

Cut rectangular according to measurements: 



_______________m²
Special cut (waterjet):



 


_______________rm

Mitre cut (45° for edges):






_______________rm
Small cuttings (< 0,7 m²):






_______________pcs.
Undercut anchor drilling for KEIL undercut anchor; hs=8.5


______​_________pcs.

Though drilling: Diameter 8 mm for rivet attachment 



______​_________pcs.
ACCESSORIES/FASTENING 

Exposed fastening with rivet
Visible attachment with rivets for aluminium substructure.
Attachment with fixed and sliding points, fixed points must be produced with sleeves. 
Attachments: Façade rivet of aluminium with head painting, head diameter 14/16mm, length depending on substructure and panel thickness.
Material: AIMg3 (material no. EN AW-5754 according to DIN EN 573-3:2003-10)
Rivet mandrel: non-corrosive steel (material no. 1.4541)
Fixed point sleeve of aluminium, outer diameter 7.7mm, length depending on panel thickness.
Material: AIMg3 (material no. EN AW-6060 according to DIN EN 573-3:2003-10)
Supplier:
Rieder Smart Elements GmbH & Co KG



Glemmerstraße 21, 5751 Maishofen, Österreich




T +43 6542 690844, office@rieder.cc, www.rieder.cc

Concealed fastening with undercut anchor
Concealed attachment with undercut anchor from Keil with setting depth 8.5mm. Screw length depending on substructure.
Approval number: ETA-06/0220
Supplier:
KEIL Befestigungstechnik GmbH



PO box 1158, 51751 Engelskirchen, Germany



T +49 2263 807 0



mail@keil.eu, www.keil.eu
Concealed fastening by bonding with Sika Tack panel system
Concealed attachment by bonding with the SikaTack panel system from Sika on uncoated aluminium.
Approval number: Z-10.8-408 (supplementary notice on the general building-supervisory approval)
Supplier:
www.sika.com
CONTACT
Sales: 

Rieder Smart Elements GmbH & Co KG
Glemmerstraße 21
5751 Maishofen
Austria
T +43 6542 690 844
office@rieder.cc 
www.rieder.cc
Production:
Rieder Faserbeton-Elemente GmbH
Bergstraße 3a
83059 Kolbermoor
Germany
T +49 8031 90167 0
office@rieder.cc 
www.rieder.cc


