

S E L E C T I O N  G U I D E  F O R  S O L D E R I N G  F L U X E S

	
	LIQUID FLUX

	
	
Appearance
	
Acid No (mg/KoH/g)
	
Flash Point
	
Solid Content wt/wt
	
Specific Gravity @25˚C
	Ph,5% V/V
aqueous Solution
	
Shelf Life
	
ROHS
	
HALO Free/ Halide Free
	
IPC-J-STD-004
Designation
	
Recommendations

	FLUX SL9000
	Physical Properties
	Clear light amber
	21
	17˚C
	4.0%
	0.793
	2.8
	3 Years
	YES
	YES
	ROLO
	Wave soldering / Select soldering

	FLUX SL900
	
	Pale Amber Liquid
	18
	13˚C
	3.9%
	0.793
	3.4
	3 Years
	YES
	NO
	ROLO
	Wave soldering / Select soldering

	FLUX SL4500
	
	Clear pale yellow Liquid
	17
	12˚C
	2.0%
	0.790
	3.3
	3 Years
	YES
	YES
	ROLO
	Wave soldering / Select soldering

	FLUX SL6300
	
	Clear light amber
	22
	12˚C
	3.6%
	0.796
	3.3
	3 Years
	YES
	NO
	ROLO
	Wave soldering / Select soldering

	FLUX SL8910
	
	Clear pale yellow Liquid
	34
	17˚C
	6.0%
	0.799
	3.1
	3 Years
	YES
	NO
	ROLO
	Wave soldering / Select soldering

	Zero Halogen ,Zero Halide Flux
	
	Clear pale yellow Liquid
	19
	14˚C
	5%
	0.793
	3.4
	3 Years
	YES
	YES
	ORLO
	Wave soldering / Select soldering

	SL-W-900 (Water soluble Flux)
	
	Water White
	19
	>13° C
	15%
	1.02
	7.0
	3 Years
	YES
	NO
	ORH1
	Wave soldering / Select soldering

	Battery Flux
	
	Clear Brown Liquid
	145
	29˚C
	45%
	1.046
	2.34
	3 Years
	NO
	NO
	ORH1
	Cast on Strap

	Solar PV Flux
	
	Pale Yellow Liquid
	15
	14˚C
	2%
	0.803
	5.0
	3 Years
	YES
	YES
	ORLO
	Photo voltaic ribbon

	Rosin Flux
	
	Light Amber liquid
	25
	14˚C
	15%
	0.825
	5.0
	3 Years
	YES
	NO
	ROLO
	Dip /Selective

	SS FLUX
	
	Pale Yellow Liquid
	35
	None
	12%
	1.500
	1
	3 Years
	YES
	NO
	ORH1
	Stainless sodlering

	Hot Air Leveling Flux
	
	Yellow Liquid
	15
	270˚C
	5%
	1.03
	2.8
	3 Years
	NO
	NO
	ORH1
	PCB manufacturing

	Radiator Flux
	
	Clear, Colorless Liquid
	25
	None
	15%
	1.2
	1
	3 Years
	NO
	NO
	ORH1
	Copper S Brass Radiators
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