S E L E C T I O N  G U I D E  F O R  S O L D E R I N G  F L U X E S

|  |  | LIQUID FLUX |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Appearance | Acid No (mg/KoH/g) | Flash Point | Solid Content wt/wt | Specific Gravity @25˚C | Ph,5% V/V aqueous Solution | Shelf Life | ROHS | HALO Free/ Halide Free | IPC-J-STD-004 Designation | Recommendations |
| FLUX SL9000 | Physical Properties | Clear light amber | 21 | 17˚C | 4.0% | 0.793 | 2.8 | 3 Years | YES | YES | ROLO | Wave soldering / Select soldering |
| FLUX SL900 |  | Pale Amber Liquid | 18 | 13˚C | 3.9% | 0.793 | 3.4 | 3 Years | YES | NO | ROLO | Wave soldering / Select soldering |
| FLUX SL4500 |  | Clear pale yellow Liquid | 17 | 12˚C | 2.0% | 0.790 | 3.3 | 3 Years | YES | YES | ROLO | Wave soldering / Select soldering |
| FLUX SL6300 |  | Clear light amber | 22 | 12˚C | 3.6% | 0.796 | 3.3 | 3 Years | YES | NO | ROLO | Wave soldering / Select soldering |
| FLUX SL8910 |  | Clear pale yellow Liquid | 34 | 17˚C | 6.0% | 0.799 | 3.1 | 3 Years | YES | NO | ROLO | Wave soldering / Select soldering |
| Zero Halogen ,Zero Halide Flux |  | Clear pale yellow Liquid | 19 | 14˚C | 5% | 0.793 | 3.4 | 3 Years | YES | YES | ORLO | Wave soldering / Select soldering |
| SL-W-900 (Water soluble Flux) |  | Water White | 19 | >13° C | 15% | 1.02 | 7.0 | 3 Years | YES | NO | ORH1 | Wave soldering / Select soldering |
| Battery Flux |  | Clear Brown Liquid | 145 | 29˚C | 45% | 1.046 | 2.34 | 3 Years | NO | NO | ORH1 | Cast on Strap |
| Solar PV Flux |  | Pale Yellow Liquid | 15 | 14˚C | 2% | 0.803 | 5.0 | 3 Years | YES | YES | ORLO | Photo voltaic ribbon |
| Rosin Flux |  | Light Amber liquid | 25 | 14˚C | 15% | 0.825 | 5.0 | 3 Years | YES | NO | ROLO | Dip /Selective |
| SS FLUX |  | Pale Yellow Liquid | 35 | None | 12% | 1.500 | 1 | 3 Years | YES | NO | ORH1 | Stainless sodlering |
| Hot Air Leveling Flux |  | Yellow Liquid | 15 | 270˚C | 5% | 1.03 | 2.8 | 3 Years | NO | NO | ORH1 | PCB manufacturing |
| Radiator Flux |  | Clear, Colorless Liquid | 25 | None | 15% | 1.2 | 1 | 3 Years | NO | NO | ORH1 | Copper S Brass Radiators |