T E C H N I C A L	D A T A	S H E E T

T E C H N I C A L	D A T A	S H E E T

SAC305 Pb Free SOLDER WIRE

## PRODUCT DESCRIPTION

SAC305 RoHS Compliance Solder Wires are being formulated with High Virgin Raw Metals Processed in state-of-the-art Technology that brings world class Quality along. Here, Oxygen interaction with Alloy is Nil and thus, Dross formulation is reduced at PCB Assembly Process. Also an increase flow rate & reduced impurities found. SAC305 Alloy is compatible for a typical range of Flux Application Formulas used in Electronics Industry Today.

## STORAGE AND HANDLING

- Do not use Fire near storage area.

- Store in Dry, Cool and Non-Corrosive environment.

- Wear Personal Protective Equipments while Handling.

- Wear Personal Protective Equipments while Processing.

## PRODUCT SPECIFICATION

| Sl No | Item | Specification | Standard |
| --- | --- | --- | --- |
| 1 | Appearance | Bright and shiny surface finishes |  |
| 2 | Alloy | Sn/Ag3.0/Cu0.5/Ni0.06/Ge0.01 | JIS-Z-3282 A CLASS |
| 3 | Melting Point | 217~2190C | DSC |
| 4 | Flux Content | 2% & 2.2% ±0.2 % | JIS-Z-3283 |
| 5 | Halide Content Under | 0.1% | JIS-Z-3283 |
| 6 | Gravity | 7.4 |  |
| 7 | Spread ability | > 80% | JIS-Z-3197 |
| 8 | Packaging | 500g, |  |
| 9 | Diameters Tolerances | 1.6mm,1mm,0.8mm,0.7mm &0.6mm ± 0.05 mm | JIS-Z-3283 |
| 10 | Flux Type | ROL1 | J-STD-004 |
| 11 | RoHS Complaint | Yes | International Standards |
| 12 | Features | Excellent solder joint reliability. Superior joint strength. Excellent thermal & Mechanical fatigue resistance. Low cleaning required after solder joint |  |
| 13 | Purpose | For use in applications requiring good activation. |  |

## PHYSICAL PROPERTIES.

| No | Test Item | Test Result | Test Method |
| --- | --- | --- | --- |
| 1 | Silver Chromate Test | PASS | IPC-TM-650, 2.6.33 |
| 2 | Copper Mirror Test | PASS | IPC-TM-650, 2.6.32 |
| 3 | Copper plate Corrosion | PASS | JIS-Z-3197, 6.6.1 |
| 4 | S.I.R Test | 1×109 up | IPC-TM-650, 2.6.3.3 |
| 5 | Electro migration Test | 1×10912up | IPC-TM-650, 2.6.14.1 |

## ALLOY COMPOSITION.

| (Sn) | (Ag) | (Cu) | (Ni) | (Ge) | (Zn) | (Al) | (Sb) | (Fe) | (As) | (Bi) | (Cd) | (Pb) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| REM. | 2.9~ 3.1 | 0.4~ 0.6 | 0.04~ 0.08 | 0.005~ 0.02 | 0.002 MAX | 0.002 MAX | 0.12 MAX | 0.02 MAX | 0.03 MAX | 0.10 MAX | 1 PPM | 100 PPM |