Leaded Solder – 63/37 - T4

# Low residue Leaded no-clean solder paste

## FEATURES

SOLDERIX Leaded range offers a good balance between wettability, printing capability and ability to withstand various thermal profiles. This range exhibits high printing speed, excellent abandon time and long steady tackiness.

These pastes can withstand high thermal profiles, with and without nitrogen, leading to consistent and shiny solder joints on all standard finishes.

Residues after reflow are non-corrosive and do not need to be removed to ensure the reliability of the PCB’s. However, those residues are easily cleanable with a large range of cleaners: hydro-carbonated solvents, halogenated solvents and detergent solutions including the SOLDERIX cleaning solutions.

## PROPERTIES

| SOLDERIX Leaded | SOLDERIX Leaded 63/37 – T3 | SOLDERIX Leaded 63/37 – T4 |
| --- | --- | --- |
| Alloy | Sn63Pb37 | Sn63Pb37 |
| Powder size distribution (microns) | 25-45 | 20-38 |
| Melting point | 183 | 183 |
| Metal content (%) | 89,5  0.5 | 89,5  0.5 |
| Residue after reflow soldering (%) | 47 – 54 | 47 – 54 |
| Halogen content | no halogen | no halogen |
| Viscosity* (Pa.s at 25°C) *Spiral pump Malcom – 10 RPM | 160 Typical value | 160 Typical value |

## CHARACTERISTICS

Long stencil life: more than 10 hrs

Abandon time on the stencil more than 4 hrs with excellent print restart

Fine pitch printing

Printing speed: 20-150 mm/sec

Solderballing resistance at high % relative humidity Good wettability on all finishes

Stable tack: more than12 hrs at 22°C between printing and component placement

Chemical reliability	6

Residue cleanliness	4

ICT Test	2

Printing speed

Stencil life

Abandon time

No slump out by preheat

Slight yellow residue after reflow, at probe compatible No halogen

0

Residue cosmetic

Tombstoning

Cold slump

Steady tack

High SIR – No residue deterioration during accelerated ageing

Compatible with major conformal coating of the market

(1) SIR/EM test at 40°C, 93 % RH, 50 V bias, 500 hours:

> 108 ohms – no dendrites

Solder beading

Wettability

Hot slump Reflow process window

| FUNCTIONAL TESTS | Results | Procedures |
| --- | --- | --- |
| Flux classification | L 0 F-SW 32 113 | ANSI/J-STD-004 DIN 8511 ISO 9454 |
| Solderballing test | class 1 | ANSI/J-STD-004 |
| Copper mirror | pass | ANSI/J-STD-004 |
| Copper corrosion | pass | ANSI/J-STD-004 |
| S.I.R. Ohms After 21 days 85°C - 85 % RH - 50 Volts End of cycle 20°C – 65°C RH | pass > 109 > 1010 | ANSI/J-STD-004 |

## PACKAGING

| Jar | 250 g or 500 g |
| --- | --- |

## STORAGE & SHELF LIFE

To ensure the best product performance, the recommended storage temperature range is 0°C to 10°C. A shelf life of 12 months is achieved under these conditions.

## PROCESS PARAMETERS

### Solder paste preparation

Before printing, it is essential to properly mix the solder paste, either manually with a spatula, or by doing several preliminary prints on the stencil.

### Printing guideline

Apply on the stencil solder paste to form a roll of 1 to 2 cm of diameter all along the squeegee (about 100g of paste per 10 cm squeegee length). This way, the solder paste will roll easily under the squeegees to offer excellent printing quality.

Printing speed   :	20 to 150 mm/sec. Minimum pitch   :	0.3 mm

Pressure	:	depends on printing speed Examples of printing speed according to the pressure :

| Squeegee length | Printing Speed | Pressure |
| --- | --- | --- |
| 250 | 50 mm/sec | 4 kg |
| 250 | 100 mm/sec | 9 kg |
| 400 | 50 mm/sec | 6 kg |
| 400 | 100 mm/sec | 11 kg |

### Reflow guideline

The graph beside indicates, the optimal thermal profile zone according to PCB and component thermal mass.

A linear preheating ramp rate is preferable to a too long soak, in order to avoid solder beading and to get a shiny joint with a uniform residue distribution.

Nitrogen atmosphere improves wettability inside a larger reflow process window.

TEMPERATURE

THERMAL PROFILE ZONE SHORT PROFILE

50-70

secs

THERMAL PROFILE ZONE SHORT PROFILE

50-70

secs

°C

240

210

180

170

160

130

20

60	120	200

TEMPERATURE

THERMAL PROFILE ZONE MEDIUM PROFIL

50-80

secs

THERMAL PROFILE ZONE MEDIUM PROFIL

50-80

secs

°C

240

210

180

170

150

140

AIR REFLOW

TIME secs

AIR REFLOW

20

60	180	260	TIME secs

TEMPERATURE

THERMAL PROFIL ZONE LONG PROFILE

50-120

secs

THERMAL PROFIL ZONE LONG PROFILE

50-120

secs

°C 240

210

18

170

140

AIR REFLOW

20

60	210

340

TIME secs

### Cleaning

After soldering, the remaining flux residue does not have to be removed by a cleaning operation as it is chemically inert. When cleaning is required (e.g. high reliability assembly, improved conformal coating adhesion), the residue left after reflow can be easily removed with a large range of cleaning solutions, such as detergents, hydro-carbonated solvents or halogenated solvents cleaning range solutions.

## HSE

Contains lead. Use in well-ventilated areas. Safety glasses and gloves should always be worn when handling the flux.