T E C H N I C A L	D A T A	S H E E T

T E C H N I C A L	D A T A	S H E E T

Sn63Pb37 Solder Wire (No Clean & Rosin Cored)

## PRODUCT DESCRIPTION

- High purity Alloy that is composed of 63% Tin and 37% Lead from Virgin Metals.

- Applies at Hand or Feed Soldering Process in Electronic & Electrical Assemblies.

- Non-Corrosive and No Impact of Residues form at Post Soldering which means of passes in Pin Probe & Flying Probe Tests for No Clean Wires.

- If requires, Residues shall clean with appropriate Liquid Application.

- Précised amount of Flux cored from state-of the-art-Technology Process.

## APPLICATION

This application is suitable for hand Soldering Process in Electronic & Electrical Assemblies. Soldering Iron Set Temperatures ranging from 350°C to 400°C are recommended to get desired Solder Joints. Application has designed with No-Clean Flux Cored in Solder & Residues may form on Joints which may contribute no impact to Circuit Assemblies. Cleaning should be done when Rosin Cored Solder Wire used.

## STORAGE AND HANDLING

  - Do not use Fire near storage area.

  - Store in Dry, Cool and Non-Corrosive environment.

  - Wear Personal Protective Equipments while Handling.

  - Wear Personal Protective Equipments while Processing.

## PRODUCT SPECIFICATION

| NO | Item | Specification | Standard |
| --- | --- | --- | --- |
| 1 | Appearance | Bright and shiny finishes | NA |
| 2 | Alloy | Sn/Pb37 | JIS-Z-3282 A CLASS |
| 3 | Melting Point | 1830C (NA for Rosin Cored Wires) | DSC |
| 4 | Flux Content | 1.3%, 1.8%,2%& 2.2% ±0.1 % | JIS-Z-3283 |
| 8 | Packaging | 500gm, |  |
| 9 | Diameter/Tolerance | 16SWG,18SWG,20SWG,22SWG,24 SWG & 26 SWG | JIS-Z-3283 |
| 11 | Features | Excellent solder joint reliability. Superior joint strength. Excellent thermal & Mechanical fatigue resistance. Low cleaning required after solder joint |  |
| 12 | Purpose | For use in applications requiring good activation. |  |

## PHYSICAL PROPERTIES.

| No | Test Item | Test Result | Test Method |
| --- | --- | --- | --- |
| 1 | Silver Chromate Test | PASS | IPC-TM-650, 2.6.33 |
| 2 | Copper Mirror Test | PASS | IPC-TM-650, 2.6.32 |
| 3 | Copper plate Corrosion | PASS | JIS-Z-3197, 6.6.1 |
| 4 | S.I.R Test | 1×109 up | IPC-TM-650, 2.6.3.3 |
| 5 | Electro migration Test | 1×10912up | IPC-TM-650, 2.6.14.1 |

## ALLOY COMPOSITION.

| (Sn) | (Pb) | (Sb) | (Cu) | (Bi) | (Zn) | (Fe) | (Al) | (As) | (Cd) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| REM | 36.5~ 37.5 | 0.12 MAX | 0.05 MAX | 0.10 MAX | 0.002 MAX | 0.02 MAX | 0.002 MAX | 0.03 MAX | 0.002 MAX |